| Item No | Item Name | Technical Specifications | Unit of Measurement | Quantity |
| --- | --- | --- | --- | --- |
| 1 | OXYGEN / NITROGEN / HYDROGEN ANALYZER | Description powerful and robust elemental analyzer for measurement of oxygen, nitrogen and hydrogen concentrations in inorganic materials like steel, iron, copper or ceramics. The highly sensitive NDIR and thermal conductivity detectors reliably detect element concentrations from low ppm content to high percentages. Features - Low gas consumption and high sensitivity due to closed gas system - Easy application of pins, powders and granules - Inexpensive argon as carrier gas possible - Short analysis time - Powerful impulse furnace with 8.5 kW - Optional Auto cleaner - Reliable ONH elemental analysis of inorganic samples like steel, non-ferrous metals, ceramics, slags, ores, etc. Technical data Measured elements: hydrogen, nitrogen, oxygen Samples: inorganic Furnace alignment: vertical Sample carrier: graphite crucibles Field of application: ceramics, engineering / electronics, steel / metallurgy Furnace: electrode impulse furnace (max. 8,5 KW*), temperatures in excess of 3,000 °C Detection method: solid state infrared absorption for oxygen thermal conductivity for nitrogen and hydrogen Typical analysis time: 120 - 180 s Chemicals required: Schuetze reagents, copper oxide, magnesium perchlorate, sodium hydroxide Gas required compressed air, helium 99.995 % pure, nitrogen 99.995% pure, argon 99.995% pure (if required), all gases with (2 - 4 bar / 30 - 60 psi) Power requirements 3~ 400 V, 50/60 Hz, max. 8,500 W Dimensions (W x H x D) 56 x 78 x 64 cm Weight~ 165 kg Required equipment: PC, monitor, balance (resolution 0.0001g) Included Articles Optional accessories: carrier gas purification, external chiller, gas calibration unit Documentation - CE marking and declaration conformity - Documents for the Installation and Operational Qualification (IQ / OQ) - Functional Specification - Design Qualification (DQ) and others relevant document | Pcs | 1 |